SECTION 071325

Self-Adhering Sheet Waterproofing

PREPRUFE® 800PA Membrane & PREPRUFE® 800PA Low Temperature Membrane

PART 1 — GENERAL

1.01 SUMMARY

A. The work of this section includes, but is not limited to, the following:

1. Non-asphaltic sheet membrane waterproofing

2. Prefabricated drainage composite

3. Protection board

B. Related Sections: Other specification sections which directly relate to the work of this section include, but are not limited to, the following:

1. Section 033000 – Cast-In-Place Concrete

2. Section 042000 – Unit Masonry

3. Section 071100 – Dampproofing

4. Section 076000 – Flashing and Sheet Metal

5. Section 079200 – Joint Sealants

6. Section 079500 – Expansion Control

7. Section 334600 – Subdrainage

1.02 SUBMITTALS

A. Product Data: Submit manufacturer’s product data, installation instructions, use limitations and recommendations. Include certification of data indicating VOC (Volatile Organic Compound) content of all components of waterproofing system.

B. Samples: Submit representative samples of the following for approval:

1. Sheet membrane

2. Protection board

3. Prefabricated drainage composite

1.03 REFERENCE STANDARDS

A. The following standards and publications are applicable to the extent referenced in the text.

B. American Society for Testing and Materials (ASTM)

C 836 Standard Specification for High Solids, Cold Liquid-Applied Elastomeric Waterproofing Membrane for Use with Separate Wearing Course

D 412 Standard Test Methods for Rubber Properties in Tension

D 570 Standard Test Method for Water Absorption of Plastics

D 882 Standard Test Methods for Tensile Properties of Thin Plastic Sheeting

D 903 Standard Test Method for Peel or Stripping Strength of Adhesive Bonds

D 1876 Standard Test Method for Peel Release of Adhesives (T-Peel)

D 1002 Standard Test Method for Apparent Shear Strength of Single-Lap-Joint Adhesively Bonded Metal Specimens by Tension Loading

D 3767 Standard Practice for Rubber - Measurements of Dimensions

D 5385 Standard Test Method for Hydrostatic Pressure Resistance of Waterproofing Membranes

E 96 Standard Test Methods for Water Vapor Transmission of Materials

E 154 Standard Test Methods for Water Vapor Retarders Used in Contact with Earth under Concrete Slabs, on Walls, or as Ground Cover

1.04 QUALITY ASSURANCE

A. Manufacturer: Sheet membrane waterproofing shall be manufactured and marketed by a firm with a minimum of 20 years’ experience in the production and sales of self-adhesive sheet membrane waterproofing. Manufacturers proposed for use but not named in these specifications shall submit evidence of ability to meet all requirements specified, and include a list of projects of similar design and complexity completed within the past 5 years.

B. Installer: A firm which has at least 3 years’ experience in work of the type required by this section.

C. Materials: For each type of material required for the work of this section, provide primary materials which are the products of one manufacturer.

D. Pre-Installation Conference: A pre-installation conference shall be held prior to commencement of field operations to establish procedures to maintain optimum working conditions and to coordinate this work with related and adjacent work. Agenda for meeting shall include review of special details and flashing.

1.05 DELIVERY, STORAGE AND HANDLING

A. Deliver materials and products in labeled packages. Store and handle in strict compliance with manufacturer’s instructions, recommendations and material safety data sheets. Protect from damage from sunlight, weather, excessive temperatures and construction operations. Remove damaged material from the site and dispose of in accordance with applicable regulations.

1. Do not double-stack pallets of membrane on the job site. Provide cover on top and all sides, allowing for adequate ventilation.

B. Sequence deliveries to avoid delays, but minimize on-site storage.

C. Safety and Handling
 Users must read and understand the product label and Safety Data Sheets (SDS’s) for each system component before use. All users must acquaint themselves with this information prior to working with the material. Carefully read detailed precaution statements on the product labels and SDS’s before use.

1.06 PROJECT CONDITIONS

A. Perform work only when existing and forecasted weather conditions are within the limits established by the manufacturer of the materials and products used.

B. Proceed with installation only when substrate construction and preparation work is complete and in condition to receive sheet membrane waterproofing.

1.07 WARRANTY

A. Sheet Membrane Waterproofing: Provide written 5 year material warranty issued by the membrane manufacturer upon completion of the work.

PART 2 — PRODUCTS

2.01 MATERIALS

A. Sheet Membrane Waterproofing: PREPRUFE® 800PA Membrane/Low Temperature Membrane as manufactured by GCP Applied Technologies; a self-adhesive, cold-applied composite sheet consisting of a thickness of 0.6 mm (0.024 in.) of synthetic non-asphaltic adhesive and 0.2 mm (0.008 in.) of multi-layer cross-laminated, high density polyethylene film specially formulated for use with the Preprufe system. Provide membrane covered with a release sheet which is removed during installation. No special adhesive or heat shall be required to form laps. Provide membrane with the following physical properties:

PHYSICAL PROPERTIES: PREPRUFE® 800PA Membrane & PREPRUFE® 800PALOW TEMPERATURE Membrane

|  |  |  |
| --- | --- | --- |
| Property | Test Method | Typical Value |
| Color |  | White |
| Thickness | ASTM D 3767 Method A | 30 mils (0.8 mm) nominal |
| Flexibility, 180° bend over 25 mm (1 in.) mandrel at -32°C (-25°F) | ASTM D 1970 | Unaffected |
| Tensile Strength, Membrane Die C | ASTM D 412 | 1000 lbs./in |
| Elongation, Ultimate Failure of SIS | ASTM D 412 | 150% minimum |
| Crack Cycling at -32°C (-25°F), 100 Cycles | ASTM C 836 | Unaffected / Pass |
| Lap Shear | ASTM D 1002 | 30 lbs./in minimum |
| Peel Strength | ASTM D 903  | 16 lbs./in. minimum  |
| Puncture Resistance, Membrane | ASTM E 154 | 100 lbs. minimum |
| Resistance to Hydrostatic Head | ASTM D 5385 |  >231 ft. of water |
| Permeance | ASTM E 96, Section 12 – Water Method | <0.1 perms |
| Water Absorption | ASTM D 570 | 0.1% maximum |

2.02 Ancillary Products – (reference gcpat.com for complete technical details)

1. Prefabricated Drainage Composite: HYDRODUCT**®** 220 and/or HYDRODUCT**®** 660 Drainage Composite as supplied by GCP Applied Technologies to promote positive drainage while serving as a protection course.

NOTE TO SPECIFIER: The following are product selection guidelines for HYDRODUCT**®** Drainage Composites. Consult the “Product Summary” and “System Components” section of the Waterproofing Systems Manual North American Edition for complete information. HYDRODUCT**®** 220: All vertical applications. HYDRODUCT**®**660: All horizontal applications. THE APPROPRIATE HYDRODUCT® DRAINAGE COMPOSITE MAY ALSO SERVE AS PROTECTION FOR ALL PREPRUFE® 800PA MEMBRANES.

1. Protection Board:
	1. 1.Expanded Polystyrene Protection Board: 25 mm (1 in.) thick for vertical applications with a Normal Density: 16 kg/m3 (1.0 lb./ft3)
	2. Asphalt Hardboard: A pre-molded semi-rigid protection board consisting of bitumen, mineral core and reinforcement.
2. Waterstop: AdcorTM hydrophilic waterstop as manufactured by GCP Applied Technologies for non-moving concrete construction joints.
3. Miscellaneous Materials: Surface conditioner, mastic, liquid membrane, tape and accessories specified or acceptable to manufacturer of sheet membrane waterproofing.

PART 3 — EXECUTION

3.01 EXAMINATION

A. The installer shall examine conditions of substrates and other conditions under which this work is to be performed and notify the contractor, in writing, of circumstances detrimental to the proper completion of the work. Do not proceed with work until unsatisfactory conditions are corrected.

3.02 SUBSTRATE PREPARATION

A. Refer to manufacturer’s literature for requirements for preparation of substrates. Surfaces shall be structurally sound and free of voids, spalled areas, loose aggregate and sharp protrusions. Remove contaminants such as grease, oil and wax from exposed surfaces. Remove dust, dirt, loose stone and debris. Use repair materials and methods which are acceptable to manufacturer of sheet membrane waterproofing.

B. Cast-In-Place Concrete Substrates:

1. Do not proceed with installation until concrete has properly cured and dried
(minimum 7-days for normal structural concrete and minimum 14-days for lightweight structural concrete).

2. Fill form tie rod holes with concrete and finish flush with surrounding surface.

3. Repair bugholes over 13 mm (0.5 in.) in length and 6 mm (0.25 in.) deep and finish flush with surrounding surface.

4. Remove scaling to sound, unaffected concrete and repair exposed area.

5. Grind irregular construction joints to suitable flush surface.

C. Masonry Substrates: Apply waterproofing over concrete block and brick with smooth trowel-cut mortar joints or parge coat.

D. Related Materials: Treat joints and install flashing as recommended by waterproofing manufacturer.

3.03 INSTALLATION

A. Refer to manufacturer’s literature for recommendations on installation, including but not limited to, the following:

1. Apply primer at rate recommended by manufacturer. Recoat areas not waterproofed if contaminated by dust. Mask and protect adjoining exposed finish surfaces to protect those surfaces from excessive application of primer.

2. Delay application of membrane until primer is completely dry. Dry time will vary with weather conditions.

3. Seal daily terminations with troweled bead of mastic.

4. Apply protection board and related materials in accordance with manufacturer’s recommendations.

3.04 CLEANING AND PROTECTION

1. Protect completed membrane waterproofing from subsequent construction activities as recommended by manufacturer.
2. Inspect for damage just prior to installation of subsequent construction activities and make repairs in accordance with manufacturer’s recommendation.